Sample: Si12 VASE with 6FDA-DAM pristine

| Fit Results MSE = 5.249 Thickness # 3 = 18.10 ± 0.017 nm E Inf = 0.767 ± 0.006764 Angle Offset = 0.0345 ± 0.004173 % Thickness Non-uniformity = 2.75 ± 0.0276 n of B-Spline @ 632.8 nm = 1.57333 | Optical Model |
| --- | --- |

Experimental and Model Generated Data Fits

Sample: Si29 VASE with 6FDA-DAM pristine

| Fit Results MSE = 24.623 Thickness # 3 = 213.30 ± 0.248 nm E Inf = 0.562 ± 0.0149 Angle Offset = -0.772 ± 0.0252 % Thickness Non-uniformity = 3.67 ± 0.0914 n of B-Spline @ 632.8 nm = 1.51720 | Optical Model |
| --- | --- |

Experimental and Model Generated Data Fits

Sample: Si6 VASE with 6FDA-DAM pristine

| Fit Results MSE = 6.126 Thickness # 3 = 32.21 ± 0.022 nm E Inf = 0.771 ± 0.006684 Angle Offset = -0.0476 ± 0.004920 % Thickness Non-uniformity = 2.80 ± 0.0288 n of B-Spline @ 632.8 nm = 1.56067 | Optical Model |
| --- | --- |

Experimental and Model Generated Data Fits

Sample: Si16 VASE with 6FDA-DAM pristine

| Fit Results MSE = 4.939 Thickness # 3 = 11.85 ± 0.015 nm E Inf = 0.737 ± 0.008649 Angle Offset = 0.0299 ± 0.003967 % Thickness Non-uniformity = 2.71 ± 0.0261 n of B-Spline @ 632.8 nm = 1.57198 | Optical Model |
| --- | --- |

Experimental and Model Generated Data Fits

Sample: Si16 VASE with 6FDA-DAM 615C pyrolyzed

| Fit Results MSE = 4.605 Thickness # 3 = 7.73 ± 0.009 nm E Inf = 0.846 ± 0.009662 Angle Offset = 0.0270 ± 0.002564 % Thickness Non-uniformity = 3.15 ± 0.0171 n of B-Spline @ 632.8 nm = 2.07525 | Optical Model |
| --- | --- |

Experimental and Model Generated Data Fits

Sample: Si29 VASE with 6FDA-DAM 615C pyrolyzed

| Fit Results MSE = 12.364 Thickness # 3 = 153.78 ± 0.142 nm E Inf = 0.745 ± 0.0151 Angle Offset = -0.311 ± 0.0159 % Thickness Non-uniformity = 2.77 ± 0.301 n of B-Spline @ 632.8 nm = 1.98606 | Optical Model |
| --- | --- |

Experimental and Model Generated Data Fits

Sample: Si12 VASE with 6FDA-DAM 615C pyrolyzed

| Fit Results MSE = 4.421 Thickness # 3 = 12.55 ± 0.009 nm E Inf = 0.835 ± 0.006069 Angle Offset = 0.0300 ± 0.002525 % Thickness Non-uniformity = 3.22 ± 0.0165 n of B-Spline @ 632.8 nm = 2.04747 | Optical Model |
| --- | --- |

Experimental and Model Generated Data Fits

Sample: Si6 VASE with 6FDA-DAM 615C pyrolyzed

| Fit Results MSE = 5.001 Thickness # 3 = 22.49 ± 0.011 nm E Inf = 0.917 ± 0.004765 Angle Offset = -0.00299 ± 0.003112 % Thickness Non-uniformity = 3.41 ± 0.0213 n of B-Spline @ 632.8 nm = 2.03904 | Optical Model |
| --- | --- |

Experimental and Model Generated Data Fits